## Slide 1: Enhancing Atomic Mobility and Desorption Kinetics in Light Metal Hydrides Tabbetha Dobbins, Rowan University, DMR 1231153
Citations
International Student
Exchange
Project ENERGY
Diffusion limitations in H
adsorption into Mg. Work of C. Steinmetz (Rowan, M.S. Student)
XRR shows 144nm ‘native’ MgH2 layer forms via inward H2 diffusion
Narase Gowda S., Ilavsky J., Gold S.A., Dobbins T., “Ultra Small Angle X-ray Scattering (USAXS) Studies of Morphological Changes in NaAlH4”, Materials Challenges in Energy, Edited by Wicks G.G., et al., 224 pp 51-60 (2010).
2. Dobbins T., Ukpai W., “A Study of the Thermodynamic Destabilization of Sodium Aluminum Hydride (NaAlH4) with Titanium Nitride (TiN) using X-ray Diffraction and Residual Gas Analysis”, Materials Challenges in Alternative and Renewable Energy: Ceramic Transactions Edited by Wicks G.G., et al. 224 pp 99-106 (2010).
3. Dobbins T., NaraseGowda S., Butler L, “Study of the Morphological Changes in MgH2 Destablized LiBH4 Systems Using Computed X-ray Microtomography”, Materials (Open Access), 5[10] pp 1740-51 (2012).
4. NaraseGowda, S., Brown C., Jenkins T., Dobbins T., “Quasi-Elastic Neutron Scattering Study of Hydrogen Dynamics in Nano-confined NaAlH4”, PRB, in preparation.
5. Dobbins T., Smith T., Lofland S., “Solid State Transformations in LiAlH4 destabilized with TiH2”, J. Alloys and Compounds, in preparation.
6. Dobbins T., Steinmetz C., Hettinger J., “Formation of a Native Hydride Layer and Its Implication to Hydrogenation of MgH2”, Int. J. Hyd. Energy, in preparation.
Solid State diffusion is enhanced in LiAlH4 when mixed with TiH2. Work of T. Smith (Rowan Univ., Undergraduate Student)
Temperature Programmed Desorption (TPD) shows release of H2 onset at 75oC in LiAlH4:TiH2 (3:1 by mol) mixtures. Pure LiAlH4 releases above Tmelt at 170oC (because convection necessary for ionic mobility).
NaAlH4 nanoconfined in Fe-BTC MOF shows significant long-range diffusion occurring at 77oC. Work of S. NaraseGowda (LaTech Univ., Ph.D.Student)
QENS shows 20% of H in long-range (slower) dynamic motion at 77oC & 127oC. 70% of H undergo localized (fast) dynamics at these temperatures.
Students from Camden County High Schools met on on Rowan’s campus for 6 Saturdays during the Fall of 2012 to learn about alternative energy and to help construct a website aimed at helping youth learn about sustainability and energy. (ProjectEnergy.net)
In the Spring semester of 2012, undergraduate students
Zachary Buck (Rowan U.)
and Shotaro
Chiba (Hokkaido U., Sappora,
JAPAN) each had
the opportunity to visit abroad
to perform
research.
Collaboration with J. Hettinger (Rowan Univ.) and A. Goudy (Delaware State Univ.)
Collaboration with S. Lofland (Rowan Univ.) and Andrew Goudy (Delaware State Univ.)
Collaboration with C. Brown (NIST/NCNR) and T. Jenkins (NIST/NCNR)
Collaboration with W. Wigfall (Rowan Univ., C.H.A.M.P.) and K. Whitehead (Rowan Univ., Dual Enrollment)
Collaboration with S. Isobe (Hokkaido Univ.)